## Slide 1
 | PCB | SUBSTRATE | DIE
M1 | 3 | 1.9 | 0.8
M2 | 2 | 1.9 | 0.8
M3 | 1 | 1.9 | 0.8
M4 | 3 | 0.9 | 0.8
M5 | 2 | 0.9 | 0.8
M6 | 1 | 0.9 | 0.8
Package dimensions (mm) |  |  | Reflow recipe (°C) |  |  | 
PCB thickness | Substrate thickness | Die thickness | Zone 4 | Zone 5 | Zone 6 | Zone 7
3 | 1.9 | 0.8 | 180 | 220 | 260 | 280
2 | 0.9 | 0.4 | 210 | 250 | 280 | 300
1 | NA | NA | 240 | 280 | 300 | 320
I haven’t finished the data with “DIE” factor involved.
So maybe you can ignore this factor since all the die thickness is 0.8.
INPUT
Package dimensions
Reflow recipe
“e.g.,”
 | ZONE 4 | ZONE 5 | ZONE 6 | ZONE 7
Recipe 1 | 180 | 220 | 260 | 280
Recipe 2 | 210 | 220 | 260 | 280
Recipe 3 | 240 | 220 | 260 | 280
Recipe 4 | 180 | 250 | 260 | 280
Recipe 5 | 210 | 250 | 260 | 280
Recipe 6 | 240 | 250 | 260 | 280
Recipe 7 | 180 | 280 | 260 | 280
.
.
.
“e.g.,”
.
.
.
.
.
.
.
.
.
.
.
.

## Slide 2
OUTPUT
All the input and output matrix is in 50 x 50 shape
Output Image file name is : IMG_1_2_3.CSV
This denotes the geometry model
So the range is 1-6
This denotes the reflow recipe
So the range is 1-81
This denotes the image sequence
So the range is 1-15